| COVER, REVISION HISTORY AND APPROVAL PAGE |  |  |
| --- | --- | --- |
| Revision No. | Brief Description of Change | Effectivity Date |
| 0 | Origination | June 10, 2019 |
| 1 | # Included “5.3. LOADING OF RAW MATERIALS and 5.7. Pump Crete Discharge”in Addition to Section 5.0 PROCEDURE & INSTRUCTIONS | September 13, 2019 |
| 2 | Added “Batching Plant, Definition of Batching Operators, and Concrete Pump Operator” in section “3.0 Definition & Abbreviations” | June 8, 2023 |
|  | Added “Batching Plant & Cistern Tank” in section “4.1 Equipment & Materials”. Revision on Responsible Person & Procedure details in section “5.1 to 5.7”. Added Concrete Batching Plant Manual in section “6.0 Appendices”. Edited the “Distribution list” in Cover, Revision History & Approval Page. |  |

|  | Name |  | Signature |
| --- | --- | --- | --- |
| Originated/ Revised by: | Richard B. Mangaoang Project Manager |  | SEE DCN |

| Reviewed by: | Sherman A. Semanero Operations Manager | SEE DCN |
| --- | --- | --- |
|  | Virtron K. Bumal-o Operations Manager | SEE DCN |
|  | Richelle D. Eslava Deputy QMR/ HR Manager | SEE DCN |

| Approved by: | Marjorie L. Olivete QMR/ Admin Director | SEE DCN |
| --- | --- | --- |
| Date Approved | June 8, 2023 |  |

Distribution List

| President/CEO | Operations Manager’s (2) | Project Manager’s (5) |
| --- | --- | --- |
| QMR/BOD’s | Admin (Common Copy) | Document Controller |

- PURPOSE AND SCOPE

To establish procedures and guidelines for the accuracy and reliability of batched ready-mix concrete at FCLDC concrete batching plant.

- REFERENCES

Simplified Construction Estimate 2000 Edition by Max b. Fajardo, UAP

ASTM C-494 Type G (Admixture)

ASTM C-39/C39M-01 (Concrete Compressive Strength Test)

- DEFINITIONS AND ABBREVIATIONS

3.1 Definitions

Concrete Mix Design - is the technical basis for the proportions of concrete mix in terms of ratios of cement, sand, coarse aggregates, admixture, and water.

Concrete Trial Mix - is the process of weighing out the various components that constitute concrete mix for tests after the details of preliminary tests and calculations required to produce concrete has been arrived at.

Ready-mix Concrete – is concrete that is manufactured in a batching plant, according to a set design mix derive from trial mix on site.

Coarse Aggregates - the portion of the aggregate used in concrete that is larger than about ³/₁₆ inch.

Fine Aggregates – the portion of the aggregate used in concrete that is smaller than about ³/₁₆ inch.

Cement - is a binder, a substance used for construction that sets, hardens, and adheres to other materials to bind them together. Cement is seldom used on its own, but rather to bind sand and gravel (aggregate) together.

Water – is a key component added to cement and aggregates to attain workability of fresh concrete.

Water-Cement Ratio - is the ratio of the weight of water to the weight of cement used in a concrete mix. A lower ratio leads to higher strength and durability, but may make the mix difficult to work with and form. Workability can be resolved with the use of plasticizers or super-plasticizers.

Admixture – a material other than water, aggregates, cementitious materials, and fiber reinforcement, used as an ingredient of a cementitious mixture to modify its freshly mixed, setting, or hardened properties and that is added to the batch before or during its mixing.

Transit Mixer – equipment uses to load and deliver the ready-mix concrete.

Backhoe – heavy equipment used to load raw materials from the stockpile to the aggregates bin.

Batching Plant - a manufacturing plant where concrete is mixed before being transported to a  construction site ready to be poured.

Batching Operators – responsible for the control of the batching plant, from loading of raw materials including their specific measurement as per specified design mixture up to the discharging of the ready-mixed concrete, also responsible for the monitoring of transit mixer.

Backhoe Operator – responsible in operating the backhoe for the loading of raw materials.

Concrete Pump Operator “Pumpcrete Operator” – responsible in operating the pumpcrete during discharge of ready-mixed concrete on site.

Transit Mixer Driver – responsible for the proper delivery of ready mix concrete from batching plant to the specific project site. He is also responsible for the cleaning of the unit.

Driver Helper – a person who serve as the assistant of the driver, he is responsible in assisting the driver during difficult maneuvers, he is also trained to operate the transit mixer for discharging the RMC on site.

3.2 Abbreviations

- RMC – Ready-mix Concrete

- ASTM - American Society for Testing and Materials

- GENERAL REQUIREMENTS

4.1    Equipment and Materials

    - Backhoe

    - Batching Plant

    - Transit Mixer

    - Water Tank / Cistern Tank

    - Aggregates

    - Cement

    - Admixture

    - Water

  - Relevant Records and Documents

    - Trial Mix Tests Results

    - Material Tests Results

    - Material Data Sheet

# 5.0	PROCEDURE & INSTRUCTIONS

# Procedure Outline

5.1.	Receiving of Batch Orders

5.2. 	Batch Material Measurement

5.3. Raw Materials Storage

5.4.	Loading of Raw Materials

5.5. Mixing of Raw Materials

5.6. Travel and Discharge of Ready-Mix Concrete

5.7. PumpCrete Discharge

5.8. Concrete Sampling

# Procedure Details

| Responsible Person | Activities | Interface Document/Person |
| --- | --- | --- |
|  | 5.1 RECEIVING OF BATCH ORDERS |  |
| Project Engineer/ Project Superintendent | - Send Electronic file or message to the batch operator to verify the schedule, volume, and availability of raw materials prior to concrete pouring - Electronic message must contain the following information; Project Name, Date and Time of Pouring, Design of RMC (Pumpcrete or Direct Pouring), Volume, and Design Strength. | Batch Operator |
| Project Engineer/ Project Superintendent | - Accomplish a READY-MIX CONCRETE REQUEST FORM to be submitted to the warehouseman of the site. | Ready Mix Concrete Request Form |
| 5.2. BATCH MATERIAL MEASUREMENT |  |  |
| Batching Operator | - Monitoring of raw materials must be done by the batching operator; in case of low stockpile the batching operator will provide purchase requisition to PLO department. | Purchase Requisition |
| 5.3. RAW MATERIALS STORAGE |  |  |
| Batch Operator / FCLDC yard Warehouseman | - Aggregates must be stored accordingly to its type; gravel and sand were stored in separate bins. All foreign material like wood, boulder or debris must be remove to avoid contamination of ready-mixed concrete. - Cement must be stored in the water tight silo - The admixture is stored in a clean stainless water tank. - The water is stored at the cistern tank |  |
| 5.4. LOADING OF RAW MATERIALS |  |  |
| Transit Mixer Driver | - The transit mixer should be parked accordingly below the central mixer of the batching plant to receive the fresh concrete that will be batched. |  |
| Backhoe Operator | - The backhoe operator fills the batching aggregates bin with fine and coarse aggregates |  |
| Batch Operator | - Specific mass of raw materials will be input in the computer (controller) as basis for the batching, this depends on the required design of the RMC. This data will be used as the recipe for the RMC. - The volume batch per transit mixer will also be input in the computer. | Design Mix Data |
| Batch Operator | - Turn on the batching equipment system. Air Compressor, Auto-greaser, Inclined Belt Conveyor, and Central Mixer will be turned on. | Batching Plant Manual |
| Backhoe Operator | - Once all the system is running, the batching plant will now start to ration the specified mass of the raw materials simultaneously. - The ration is sufficient for ½ cubic meter of fresh concrete or 1 cycle. |  |
| Backhoe Operator | - After the rationing of the raw materials, the system will automatically send all these raw materials into the central mixer. |  |
|  | 5.5. MIXING OF RAW MATERIALS |  |
| Batch Operator | - The central mixer will then mix these raw materials for 20-30 seconds. - After mixing, the system will automatically open the discharge gate of the central mixer. - Slump testing will be conducted if necessary. |  |
| Transit Mixer Driver | - The transit mixer which drum is rotating in idle mode will now receive the fresh concrete. |  |
|  | 5.6. TRAVEL AND DISCHARGE OF READY-MIX CONCRETE |  |
| Transit Mixer Driver | - The transit mixer with RMC will be travelled to the specified site project at least within 1 hour in order not to compromise the quality of mixture. | Concrete Delivery Form / Concrete Test Report |
| Project Engineer | - Upon arrival on site, the mixture will be mixed into a higher rpm and if necessary, admixture or water will be added to attain the desired concrete mixture. - Slump testing will be conducted prior to discharge of RMC. | Concrete Delivery Form / Concrete Test Report / Pouring Request Form |
| Transit Mixer Driver Assistant | - If the desired mixture is attained on site, the concrete will be discharge either by direct pouring or concrete pump. |  |
|  | 5.7 PUMPCRETE DISCHARGE |  |
| Pumpcrete Operator and Personnel | - If the RMC will be discharged using a concrete pump equipment, the pump must be set-up the day before the pouring schedule. |  |
|  | 5.8 CONCRETE SAMPLING |  |
| Project Engineer | - Slump testing will be done on site to verify mixture workability. In any case the ideal slump was not met, the concrete engineer of the site may add partial water or admixture for low slump result, for high slump result the engineer may add cement on site. - Concrete cylinder sample will also be taken upon discharging half load of the RMC . | Concrete Delivery Form / Concrete Test Report |

# 6.0	APPENDICES

PM-OPN-02-01 - Pouring Request Form

FM-OPN-07-01 – Delivery Receipt (Ready Mix)

FM-OPN-07-02 - Ready Mix Concrete Request Form

PM-OPN-02-19 - Concrete Cylinder Test Summary Register

PM-OPN-02-07 - Testing Log Sheet

Concrete Test Report ( Third Party )

Concrete Batching Plant Manual